## Slide 1
The ability to thermally trigger a conformational change
and collapse in a constituent resilin-like protein (RLP) provides
the opportunity to build, and eventually move, a bundlemer nanostructure.
Bundlemer peptides can still assemble into coiled coil bundles even with RLPs attached to all four constituent peptides in each bundle.
This is a clear demonstration that biosynthesis can be used for bundlemer building block production for future study.
This ability affords a mechanism for the formation (and disassembly) of bundlemer-based nanomaterials through temperature responsive proteins
The ability to thermally trigger a conformational change/collapse in a constituent polymer/protein provides the opportunity to purposefully move a bundlemer nanostructure in future Aim 2 efforts.
This is a major step towards success of Aim 2 in which nanostructures will be purposefully moved. The thermal collapse of the RLP can be used to both form structure (Aim 1) and to move structure (Aim 2).
The successful biosynthesis from E. Coli of the bundlemer peptide and RLP constructs clearly affords future success in peptide/protein production with biosynthesis for scale up and study.
University of Delaware MRSEC
DMR-2011824
One-dimensional fibrillar assemblies from bundlemer coiled coil building blocks with thermoresponsive resilin-like protein (RLP) end groups. At low temperature, the RLPs collapse and aggregate forming the 1-D structure due to the bundlemer cylindrical shape. CryoTEM shows same nanostructure in all four samples with four short RLP sequences on each bundlemer end (A, B) or longer RLP end groups (C, D). Scale bars 500 nm. (E) Coarse-grained simulation of RLPs (blue) assembling together with bundlemer peptides (yellow) lining up in a 1-dimensional fashion.
Genetic Fusion of Thermoresponsive Polypeptides Mediates 1-D Assembly of Coiled Coil Bundlemers
Sai Patkar*, Yao Tang*, Darrin Pochan*, Kristi Kiick*,#, *Materials Science and Engineering, #Biomedical Engineering
Tianren Zhang*,@, Jeffrey Saven@, @Chemistry, University of Pennsylvania
Notes: What Has Been Achieved: This work is definitive demonstration that i) the termini of bundlemer forming peptides can be genetically fused with a variety of thermoresponsive peptides biosynthesized from E. Coli in significant yields. Furthermore, the assembly of the nanostructure is triggered with temperature to control the thermoresponsive resilin-like polypeptide with the bundles providing the 1-D propensity.
Importance of the Achievement: This is an important step in the triggered formation of nanostructure (Aim 1) and to show viability of moving nanostructure with thermoresponsiveness in Aim 2.
How is the achievement related to the IRG, and how does it help it achieve its goals? These results show that A) bundlemer-protein constructs can be directly biosynthesized and correctly assembled in aqueous solution. This reveals the feasibility of biosynthesis of other constructs to impact all Aims going forward and B) responsive proteins can respond as expected (in this case, with respect to temperature) even when conjugated to bundlemer sequences.
Where the findings are published: Patkar, S.S.; et al., Genetic Fusion of Thermoresponsive Polypeptides with UCST-type Behavior Mediates 1D Assembly of Coiled-Coil Bundlemers. Angewandte Chemie, 2023, in press, DOI: 10.1002/202301331