## Slide 1
Atomic-scale origin of the low grain-boundary resistance in perovskite solid electrolyte Li0.375Sr0.4375Ta0.75Zr0.25O3
UCI MRSEC
DMR-2011967
T. Lee, C.A. Gadre, H. Huyan, C. Du, J. Li, T. Aoki, R. Wu, X. Pan (University of California, Irvine)
J. Qi, S. Ko, Y. Zuo, J. Luo, S. P. Ong (University of California, San Diego)
Atomic-scale study of the crystal structure inside the grain bulk, a (010) faceted grain boundary (GB), and non-faceted general GBs.
The main achievement of this research is revealing the atomic-scale origin of the low grain-boundary (GB) resistance in Li0.375Sr0.4375Ta0.75Zr0.25O3 (LSTZ0.75) perovskite solid electrolyte and providing insights on overcoming the ubiquitous bottleneck of high GB resistance in other oxide solid electrolytes.
Significance of this scientific achievement
· Aberration-corrected scanning transmission electron microscopy and spectroscopy, along with an active learning moment tensor potential, were used to reveal the atomic scale structure and composition of LSTZ0.75 GBs.
· Li depletion, which is a major cause for the low GB ionic conductivity of Li3xLa2/3-xTiO3 (LLTO), was found to be absent for the GBs of LSTZ0.75.
· A unique defective cubic perovskite interfacial structure that contained abundant vacancies was discovered at the GBs of LSTZ0.75. The authors attributed the low GB resistance of LSTZ0.75 to this microstructure.
· Based on these results, the authors conclude vacancy and defect engineering can effectively improve GB ionic conductivity of solid Li-ion conductors, given that the material’s original structural framework should be maintained.
Contribution to IRG 1
This study provides new insights into the atomic-scale mechanisms of low GB resistance and sheds light on possible paths for designing compositionally complex oxide solid electrolytes with high total ionic conductivity.
2023 IRG-1 Intellectual Merit
Lee T, Qi J, Gadre CA, Huyan H, Ko S-T, Zuo Y, Du C, Li J, Aoki T, Wu R, Luo J, Ong SP, Pan X. “Atomic-scale origin of the low grain-boundary resistance in perovskite solid electrolyte Li0.375Sr0.4375Ta0.75Zr0.25O3”. Nature Communications, 14, 1940 (2023). https://doi.org/10.1038/s41467-023-37115-6
Notes: What Has Been Achieved: An additional achievement is the discovery of structural ordering in grain bulk of LSTZ0.75. The selected area electron diffraction (SAED) collected from grain bulk exhibits superlattice spots that had failed to be observed in the corresponding FFT pattern. This indicates the existence of short coherence length ordering in LSTZ grain bulk.
Importance of the Achievement: Further MD simulations show that activation energies (Ea) decrease and room temperature ionic conductivities () increase with increasing disorder. With the SAED results indicating the existence of short coherence length A-site ordering in LSTZ grain bulk and the trend uncovered by simulations, we believe the of LSTZ can be further enhanced by promoting disorder in A-sites.
How is the achievement related to the IRG, and how does it help it achieve its goals? One of the missions of IRG 1 is to understand how structural, chemical, and electronic nanoscale disorder of interfaces in compositionally complex materials relates to emergent macroscopic functional and mechanical behavior, such as improved conductivity and strength. This study establishes an important understanding in the base material of the compositionally complex material that we have further studied. In our other study, we establish compositionally complex perovskite oxides as a new class of Li-ion solid electrolytes and further contributes to the mission of IRG 1.
Where the findings are published: This work has been accepted in Nature Communications.
Detailed figure caption:
Atomic-scale study of the crystal structure inside the grain bulk, a (010) faceted grain boundary (GB), and non-faceted general GBs. a, Atomic-resolution HAADF-STEM image of a (010) faceted GB (with respect to the left-side grain). The zone axes parallel with the incident electron beam were indicated in a, f, and g. b, FFT pattern of the crystal structure inside the grain, boxed in blue in a, and c, FFT pattern of superlattice structure near (010) faceted GB, boxed in red in a. The , , and superlattice spots associated with the long coherence ordering in the (010) plane were circled in green. d, SAED pattern of LSTZ0.75 grain bulk along the [100] zone axis. The , , , , , and diffraction spots failed to be observed in the corresponding FFT pattern were circled in red. e, SAED pattern of superlattice structure near (010) faceted GB along the [100] zone axis. The , , and diffraction spots failed to be observed in the corresponding FFT pattern were circled in red. f, g, Atomic-resolution HAADF-STEM images of general GBs. The left-side grain in f was not oriented along any particular zone axis.
What Has Been Achieved: An additional achievement is the discovery of structural ordering in grain bulk of LSTZ0.75. The selected area electron diffraction (SAED) collected from grain bulk exhibits superlattice spots that had failed to be observed in the corresponding FFT pattern. This indicates the existence of short coherence length ordering in LSTZ grain bulk.
Importance of the Achievement: Further MD simulations show that activation energies (Ea) decrease and room temperature ionic conductivities (𝜎_(300 K)) increase with increasing disorder. With the SAED results indicating the existence of short coherence length A-site ordering in LSTZ grain bulk and the trend uncovered by simulations, we believe the 𝜎_b of LSTZ can be further enhanced by promoting disorder in A-sites.
How is the achievement related to the IRG, and how does it help it achieve its goals? One of the missions of IRG 1 is to understand how structural, chemical, and electronic nanoscale disorder of interfaces in compositionally complex materials relates to emergent macroscopic functional and mechanical behavior, such as improved conductivity and strength. Our study establishes an important understanding in the base material of the compositionally complex material that we have further studied. In our other study, we establish compositionally complex perovskite oxides as a new class of li-ion solid electrolytes and directly contributes to the mission of IRG 1.
Where the findings are published: This work has been accepted in Nature Communications.