## Slide 1: Chemically-Triggered Synthesis, Remodeling, and Degradation of Soft Materials
Typical polymers, such as those used in plastics, are static structures whose material properties are not readily manipulated. Further, most plastics cannot degrade, and thus accumulate in the environment.
This works demonstrated a series of morphological changes could be induced with a small set of monomers due to the use of reversible covalent bonding interactions.
Amphiphilic polymers, hydrogels, hydrophobic entities, and cross-linked matrices, could be all be interchanged by the addition of simple chemical triggers.
Differences in rheology, strength, as well as gelling and optical properties, were easily controlled and manipulated with the chemical triggers.
Finally, and maybe most significant, all the macromolecular structures were easily and rapidly converted (degraded) into small organic compounds with the treatment of a single chemical trigger.
MRSEC: DMR-1720595
2020
E. Anslyn, N. Lynd: Univ. of Texas at Austin
[X. Sun, M. Chwatko, D.-H. Lee, J. L. Bachman, J. F. Reuther, N. A. Lynd, and E. V. Anslyn, J. Am. Chem. Soc. 142, 3913-22 (2020).]
Notes: Polymer topology dictates dynamic and mechanical properties of materials. For most polymers, topology is a static characteristic. In this work, we presented a strategy to chemically trigger dynamic topology changes in polymers in response to specific chemical stimulus. Starting with a dimerized PEG and hydrophobic linear materials, a lightly cross-linked polymer, and a cross-linked hydrogel, transformations into an amphiphilic linear polymer, lightly cross-linked and linear random copolymers, a cross-linked polymer, and three different hydrogel matrixes, were achieved via two controllable cross-linking reactions: reversible conjugate additions and thiol-disulfide exchange. Significantly, all the polymers, before or after morphological changes, can be triggered to degrade into thiol- or amine-terminated small molecules. The controllable transformations of polymeric morphologies and their degradation heralds a new generation of smart materials.
Publication citation for this work:
X. Sun, M. Chwatko, D.-H. Lee, J. L. Bachman, J. F. Reuther, N. A. Lynd, and E. V. Anslyn, J. Am. Chem. Soc. 142, 3913-22 (2020).