## Slide 1
Harnessing moiré ferroelectricity to modulate light emission from a semiconductor monolayer
UT-Austin MRSEC
DMR- 2308817
Li and Shih at UT-Austin + Miyahara at Texas State Univ (PREM)
A heterostructure consisting of a twisted hBN substrate and a semiconductor functional layer has been built, combining the properties of the two components
Twisted hBN substrates leads to ferroelectric domains due to inversion symmetry breaking at the interface; the electrostatic potential on the top surface may be used to modify properties of an adjacent layer
In the plane electric field at the domain walls separate the electron-hole pair and induces Stark shifted excitons
A global gate can erase and restore ferroelectric domains, leading to hysteresis and switching in light emission.
A demonstration of using remote moiré potential to modulate a functional layer, a key goal of the IRG 2
(a) Illustration of how the remote potential from twisted hBN modulates a functional layer. (b) optical image of heterostructure and Kelvin probe force microscopy image of twisted hBN, (c) optical spectra taken from three locations, the middle one is taken at a domain wall; (d) in-plane E-field induces Stark shift; (e) electric gate erases and restores ferroelectric domains. (f) electric field switching of light emission; (g) illustration of spectral and spatial modulation of light emission in vdW heterostructure
Kim et.al Under review
Twisted hBN
Functional layer
(a)
(b)
(c)
(d)
(e)
(f)
(g)
Notes: What Has Been Achieved: We show that ferroelectric polar domains formed in a twisted hexagonal boron nitride (t-hBN) substrate can modulate light emission from an adjacent semiconductor monolayer. The abrupt change in electrostatic potential across the domains produces an in-plane electric field (E-field) and leads to a remarkably large exciton Stark shift in the adjacent MoSe2 monolayer, previously only observable in p-n junctions created by the advanced e-beam lithography tools. Both the spectrum and spatial pattern of the light emission of the monolayer are periodically modulated by the remote moire potential imposed by the t-hBN substrate.
Importance of the Achievement: Ferroelectricity has been recently discovered in stacked or twisted van der Waals (vdW) layers. The versatility of producing a large array of size-tunable domains and integration with diverse functional materials make them an enticing platform for developing multifunctional devices. Here, we show that ferroelectric polar domains formed in a twisted hexagonal boron nitride (t-hBN) substrate can modulate light emission from an adjacent semiconductor monolayer.
How is the achievement related to the IRG, and how does it help it achieve its goals? One key goal of IRG 2 is to extend the strategy of moire engineering to a broader range of materials using the concept of remote potential engineering. This work represents the first demonstration of combining the functionality of a moire substrate and the light emission properties of a semiconductor monolayer.
Where the findings are published: Under review at Nature Nanotechnology
What Has Been Achieved: The researchers used scanning tunneling microscopy spectroscopy (STM/S) and nano-ARPES to investigate electronic structures of 30° twisted bilayer WSe2 moiré quasicrystals and 21.8° twisted bilayer WSe2 moiré crystals. The former featured an aperiodic long-range order that yield a dense set of diffraction spots in the k space. The VHS signatures originating from several mini-gaps in the quasiperiodic structure were observed that can be explained using a coupled K-valley model with up to third-order Umklapp scattering suggesting strong interlayer coupling. For the commensurate 21.8° (38.2°) structure, two points in the moiré Brillion zone of interest were the anti-crossing at the μ point and the coherent coupling at κ point, which were also probed by the unique technique: constant current STS. In contrast to the previously studied 30° twisted bilayer graphene, the flatter dispersion of our system leads to stronger interlayer coupling at a smaller bias voltage making it a very promising platform to study the physics of moiré quasicrystals at finite doping and gating.
Importance of the Achievement: TMD-based moiré quasicrystals is a semiconductor system with strong spin–orbit coupling that endows a rich interplay of valley and spin degrees of freedom that affect both optical and transport properties. The theoretical analysis further shows that such moiré quasicrystals can be generalized to multilayer structures with higher rotational symmetry in which the quasiperiodic interlayer coupling can be brought down in energy even further. For example, using trilayers with two consecutive 20° twists, a previously unknown type of quasicrystal with 18-fold rotational symmetry and with an even denser set of diffraction patterns in which the mini-gaps are expected to occur at smaller doping. This work provides a proof of concept for using large-twist-angle vdW structures as a design platform to explore moiré physics beyond those formed at small twist angles.
How is the achievement related to the IRG, and how does it help it achieve its goals? This study demonstrate the rich electronic structures in large angle twisted bilayer WSe2 exemplified by the formation of multiple mini-gaps near the valence band maximum. By tuning the commensurability, the moiré material properties and functionalities can be precisely engineered. Moreover, by tailoring the band dispersion of the moiré crystals and quasicrystals at large twist angles, it paves the road for the further study of gate tunable electron correlation and photonic structures that harness the unique properties of moiré materials. This exactly matches the goal of IRG2. After this work, more related collaborations in optical and transport studies of the same systems are on going at UT Austin.
Where the findings are published: Nature volume 625, pages494–499 (2024) DOI: 10.1038/s41586-023-06904-w