## Slide 1
MEM-C IRG-1: Patterning Nanocrystals on Photonic Cavities
with Electrohydrodynamic Inkjet Printing
Devin MacKenzie, Daniel Gamelin, Christine Luscombe,
Jim De Yoreo, Arka Majumdar
Electrohydrodynamic ink jet printing has been used to print CsPbBr3 nanocrystals into very small features, with spot sizes down to only a few hundred nanometers across. The nanocrystals survive the printing, and even spontaneously self-organize into superlattices. This printing method allows deterministic placement of the nanocrystals onto various kinds of surfaces. For example, using this method, it was possible to print CsPbBr3 nanocrystals onto photonic cavities, which then showed sharp cavity-coupled emission at its grating ends.
These results demonstrate a powerful approach to integrating colloidal nanocrystals into complex architectures to create entirely new photonic structures. The approach is versatile and can be adapted to print other nanocrystals developed by MEM-C's IRG-1 to form new heirarchical structures, helping this MRSEC achieve its goals of exploiting the photonic properties of defects in colloidal nanocrystals to advance future technologies.
Electrohydrodynamic ink jet printing of colloidal CsPbBr3 nanocrystals. Spot sizes down to only a few hundred nanometers can be achieved with excellent spatial positioning. Using this method, CsPbBr3 nanocrystals were printed onto photonic cavities, which then showed sharp cavity-coupled emission at their grating ends.
U. Washington MRSEC
DMR-1719797
Notes: What Has Been Achieved: Electrohydrodynamic (EHD) inkjet printing was used to deterministically position CsPbBr3 NCs on nanophotonic structures. Atomic force microscopy (AFM) images and photoluminescence (PL) studies of printed NCs showed that tunable NC features with diameters of 500 nm and heights of 50 nm could be reproducibly fabricated without compromising the NCs’ PL properties. We used silicon nitride membrane transmission electron microscopy (TEM) grids to collect the first high-resolution TEM images of EHD printed NCs to date. These images showed that in some cases, 200 nm printed features containing < 200 individual NCs can be fabricated with EHD inkjet printing. Finally, we demonstrated that this printing method can deterministically place these NCs onto silicon nitride nanobeam cavities with NC emission successfully coupled to the cavity modes.
Importance of the Achievement: These results demonstrate EHD inkjet printing as a scalable, precise method to pattern luminescent nanomaterials for photonic applications. These results also demonstrate that EHD inkjet printing is compatible with the demands of lead-halide perovskite nanocrystals, which may be easily degraded during processing.
How is the achievement related to the IRG, and how does it help it achieve its goals? This work provides proof-of-concept results showing the feasibility of translating IRG-1's innovations in nanocrystal development into the realm of photonics applications. Such proof-of-concept device-level demonstrations help to motivate the use-inspired basic research activities of the IRG, in this case validating the development of light-emitting colloidal nanostructures for photonics.
Where the findings are published: Cohen, T. A.; Sharp, D.; Kluherz, K. T.; Chen, Y.; Munley, C.; Anderson, R. T.; Swanson, C. J.; De Yoreo, J. J.; Luscombe, C. K.; Majumdar, A.; Gamelin, D. R.; Mackenzie, J. D. “Direct Patterning of Perovskite Nanocrystals on Nanophotonic Cavities with Electrohydrodynamic Inkjet Printing.” Nano Letters, 2022, 14, 5681–5688. DOI: https://doi.org/10.1021/acs.nanolett.2c00473